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Factory Supply High Purity Aluminium Stearate Powder with Competitive Price

1. Product introduction:

Aluminium Stearate
CAS Number: 637-12-7 
Molecular formula: C54H105AlO6 
Molecular weight: 877.40


3. Product specification:
 
	Assay item
	Unit
	Standard Index

	Appearance
	/
	White Powder

	Aluminium Content
	%
	4.0-5.2

	Free Acid
	%
	≤6.0

	Heating loss
	%
	≤1.50

	Melting Point
	0C
	155-170

	Fineness(200 mesh)
	%
	≥99.0
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4. Application:

a.It can be used as raw material for the manufacture of metal rust inhibitor.

b.It can be used as a waterproofing agent for building materials, a brightening and thickening agent for coatings and inks. 

c.It is used as an emulsifier for cosmetics and a lubricant for plastics, etc. 

d.It can also be used as a heat stabilizer for polyvinyl chloride.
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Package: 25Kg per paper bag, with inner PE bag. 
Storage: In cool and draught place, no exposure to moisture, heat, fire or corrosion, not pile with acid, Bases and corrosion goods.

[image: 下方插入段落][image: 上方插入段落]​[image: 12294543664]
XIAMEN DITAI CHEMICALS CO., LTD
8FL,Hongsheng Building,West Hexiang Road,Xiamen, China
ISO9001:2015  Certificated 

image1.png




image2.jpeg




image3.jpeg




